Product Information Bulletin

A400 TAC SOLVENT FREE VOC COMPLIANT MODULAR CARPET TILE ADHESIVE

DESCRIPTION:

A400 Tac is a low odour, solvent free, VOC compliant, pressure sensitive adhesive.  This adhesive is specifically formulated for use with most types of modular carpet tiles.  A400 Tac can be used to install the above tiles to most common interior sub-floors.

CHARACTERISTICS

* Water based

* Solvent free

* VOC Compliant

* Low odour

* Spreads easily

* Economical

* Pressure sensitive

* Dry time; 20-30 minutes

* Coverage; 10-15m²/ltr

* Available in; 15ltr & 4ltr pails

SURFACE PREPARATION

All sub-floor surfaces shall be dry, smooth, sound and clean, free of wax, grease and all other contaminants that inhibit adequate adhesion to the sub-floor.  The sub-floor must also be free from hydrostatic pressure or capillary action.  The adhesive should not be used in excessive cold or hot conditions i.e. below 8(c or above 28(c.

It is recommended that highly porous timber or concrete sub-floor surfaces be primed with Primer 44 and allowed to cure before applying adhesive. Uneven or damaged floors should be repaired with a cementitious levelling compound.

Timber sub-floors should be tested with an appropriate electrical resistance meter. The timber sub-floor should contain a maximum moisture content of 12%. Particle board flooring requires sanding to remove the wax sealer, prior to the use of this adhesive.  All concrete sub-floors should be tested for relative humidity (RH) prior to surface priming or application of adhesive. Ensure the RH (use insitu probe method ASTM F2170 current version) of the concrete sub-floor does not exceed 75%. Also ensure the surface pH of the concrete sub-floor is less than 9. Burnished concrete sub-floors must be ground back to allow for sufficient porosity and adhesion to the sub-floor.

If the sub-floor exceeds the recommended RH & pH  levels, sufficient remediation is required prior to the use of this adhesive.  All sub-floors should in accordance with current Australian Standard installation practices.

APPLICATION

Stir the adhesive prior to use, apply the adhesive with either a U1 trowel or a medium napped paint roller. Apply an even coat weight of adhesive to the sub-floor.  Spread as much adhesive as desired & allow the adhesive to dry.  The adhesive will change from a bright blue colour when wet to a dull blue colour when dry.  This tack remains indefinitely, providing the adhesive is free from dust. Install the modular carpet tiles onto the sub-floor when the adhesive has dried. Complete the installation in accordance with the Carpet tile manufacturer’s installation instructions.

CLEAN UP

Clean tools and equipment immediately with warm soapy water.  To remove dried adhesive, use Holdfast Super Cleaning Solvent.

CAUTION

Do not allow adhesive to freeze, unaffected by freezing when dry. This adhesive has a shelf life of 12 months from date of manufacture kept in a unopened container under cover at 20°C.

VENTILATION

Always make sure that there is adequate ventilation when using this adhesive.

CONDITIONS OF SALE:  contain a limited warranty against manufacturing defects.

# NOTICE TO THE PURCHASER

All statements and technical information contained herein are based on tests we believe to be reliable but the accuracy thereof is not guaranteed.  Users assume all risk and liability resulting from the use of this product and must confirm the suitability thereof by their own tests.

CONTACT POINT:		Technical Manager

TELEPHONE:		(03) 9797 1888

# Text boxes

September

2014