Product Information Bulletin

ECO-GRAB 640 MODULAR CARPET TILE ADHESIVE

DESCRIPTION:

640 is a solvent free, VOC compliant, pressure sensitive adhesive.  This adhesive is specifically formulated for use with most types of modular cushioned backed carpet tiles.  This adhesive may be used over most common interior concrete and wooden sub-floors. 640 is also suitable to be applied over existing adhesives that remain well bonded to the sub-floor and non friable.

CHARACTERISTICS

* RH resistance 85% and falling

* Water based

* Solvent free

* VOC Compliant

* Minimal floor preparation

* Pressure sensitive

* Dry time; 20-30 minutes

* Coverage; 5-7m²/ltr

* Available in; 15ltr pails

* Blend of synthetic polymers

SURFACE PREPARATION

All sub-floor surfaces shall be dry, smooth, sound and clean, free of wax, grease, oil, laitance, bond breakers and all other contaminants that inhibit adequate adhesion.  The sub-floor must also be free from hydrostatic pressure or capillary action.  The adhesive should not be used in excessive cold or hot conditions i.e. below 8(c or above 28(c.

Uneven or damaged floors should be repaired with a cementitious levelling compound.  All subfloors should be tested for moisture content prior to application of this adhesive. The moisture content of the sub-floor should not exceed 85% relative humidity (in slab probe ASTM F2170 method). The pH of the sub-floor should not exceed 9. Do not use this adhesive if the relative humidity and pH levels are above the acceptable standards. All subfloors should be in accordance with current Australian standard installation practices.

APPLICATION

Apply the adhesive with a medium napped paint roller. Apply an even coat weight of adhesive to the sub-floor.  Spread as much adhesive as desired & allow the adhesive to dry.  The adhesive will change from a white colour when wet to a transparent colour when dry.  This tack remains indefinitely, providing the adhesive is free from dust. Install the modular carpet tiles onto the sub-floor when the adhesive has dried. Complete the installation in accordance with the carpet tile manufacturer’s installation instructions.

CLEAN UP

Clean tools and equipment immediately with warm soapy water. To remove dried adhesive, use Holdfast Super Cleaning Solvent.

CAUTION

Do not allow adhesive to freeze, unaffected by freezing when dry. This adhesive has a shelf life of 12 months from date of manufacture kept in a unopened container under cover at 20°C.

VENTILATION

Always make sure that there is adequate ventilation when using this adhesive.

CONDITIONS OF SALE:  contain a limited warranty against manufacturing defects.

# NOTICE TO THE PURCHASER

All statements and technical information contained herein are based on tests we believe to be reliable but the accuracy thereof is not guaranteed. Users assume all risk and liability resulting from the use of this product and must confirm the suitability thereof by their own tests.

CONTACT POINT:		Technical Manager

TELEPHONE:		(03) 9797 1888

# Text boxes

September

2014